## Slide 1: MSE 593 Data-Driven Materials Design and Genomics
Professor Wenhao Sun whsun@umich.edu
2023 Hokkaido Summer School
Data-Driven Computational Materials Design:
Lecture 2: Materials Project and Pymatgen
Notes: Syllabus Wenhao Sun
Set up Canvas – Katsuyo
Google Survey – Katusyo

## Slide 2
Cross-Industry Standard Process for Data Mining
(CRISP-DM)
Materials
Lecture 2

## Slide 4
Go to www.materialsproject.org
Create an account
Explore Fe
Explore GaN
Explore others
Explore Crystal Toolkit
Important Aspects
Navigating search results
Crystal Structure in DFT
E_above_hull
mp-id
A tour of the MaterialsProject

## Slide 5
Lots of things to explore!

## Slide 6
Before 2010 – DFT studies on single materials systems
Today
It’s not just ‘more’ data, you can do a different kind of science:
Visualize broad chemical trends
Quantitative statistics
Fast prototyping and Broad hypothesis testing
Materials Search
1400 data points
30,000 data points
6,000 data points
2011 – Materials Genome Initiative, Materials Project
For Loop

## Slide 7
Density Functional Theory is a
first-principles
atomistic theory
that can approximately calculate
the energy and electronic structure
of a unit cell with periodic boundary conditions
of generally fewer than 100 atoms

## Slide 8
Kinetic Energy
External Potential
e- - e- Interaction
TOO EXPENSIVE!
Can only solve about 10 Electrons = 1 Atom of Neon

## Slide 9
Electron Density
n(R)
Energy of System
E0
External Potential
(Crystal Structure + Number of e-)
Sort of …

## Slide 10: Approximations for E[n(R)]
Functional | Local Density Approx. (LDA) | Generalized Gradient (GGA) | Hybrid (B3LYP, HSE)
Approximation | Constant Electron Density | Gradient Electron Density | GGA + Exact XC
Energy Errors | ± 10 kJ/mol | ± 10 kJ/mol | ± 3 kJ/mol
Band Gap | 40-100% Under | 40-100% Under | ± 10%
Band Structure | 15% Error | 15% Error | 1% Error
Computational Cost | Good | Good | 100x GGA/LDA

## Slide 11: Practical Considerations for DFT
Unit Cell
w/ Periodic Boundaries
Bulk: Crystal Structure
Supercell: minimize short-range effects
2 atoms : 10 seconds on 1 CPU
80 atoms : 18 hours on 16 CPUs
1000 atoms : 1 month on 1000 CPUs
Computer Time scales as O(n3)
Calculation Parameters
Convergence vs. Computational Cost
Parameters
# of K-points
Energy cutoff for Basis Functions
Functional Used
Precision costs time
S.E.C = Standard Energy Calculation
Band Structure = 2-3 x S.E.C
Magnetic Calculation = 5-10 x S.E.C.
High Precision HSE = 100 x S.E.C.

## Slide 12
DFT in Computational Materials Design
DFT Inputs
Crystal Structure
Known structures:
(ICSD) Inorganic Crystal
Structure Database
New Structures:
Chemical substitutions
Crystal structure prediction
Defect Structures:
Slabs, Vacancies, Dislocations
Strained, Distorted
DFT Outputs
Phase Stability
Formation Energies
Vibrational entropies
Reaction Energies
Band Structure
Band Gap,
Effective Mass
Dielectric constant
Defect Energies
Surface energies
Dislocation energies
Mechanical Properties
Elastic Tensors
Gruneisen Parameter
Speed of sound
Transport Properties
Diffusion constants
Structure 
Property Screen
 Parameters for
Multiscale Modeling 

## Slide 13: Thermodynamics
Crystal Structure Prediction
Phase Diagrams + Reactions
Lowest Energy Structure is the Winner!
AgAu2F8, BaFe2Br8, BaFe2Br8, BaMn2O8, BaTm2F8, BeB2H8, BeB2H8, CaB2F8, , CdAl2Cl8, CdAu2F8, CeSe2O8, CoAl2Cl8, CoCl2O8, CuAl2Cl8, CuAl2Cl8_p1, CuAl2Cl8, CuGa2Cl8, HfMo2O8, HgAu2F8, MgAl2Cl8, MgAu2F8, MnB2F8, MoU2O8, MoV2O8, MoV2O8, NiAu2F8, NiAu2F8, NiAu2F8, NiCl2O8, PdAl2Cl8, PdAu2F8, PdAu2F8, PdGa2Br8, PdGa2I8, …etc etc

## Slide 14: Kinetics
Surface Energies, Surface Reconstructions, Nanoparticle Morphologies
Diffusion Energy Barriers – Diffusion Paths

## Slide 15: Electronic Structure

## Slide 16: Mechanical Properties

## Slide 17
Density Functional Theory is a
first-principles
atomistic theory
that can approximately calculate
the energy and electronic structure
of a unit cell with periodic boundary conditions
of generally fewer than 100 atoms

## Slide 18: Computational MSE spans multi-hierarchical length and time scales
DFT
Input:
Chemistry
Crystal Structure
Output:
Formation energies
Elastic Constant
Thermal Expansion
Calphad: Phase Diagram
Processing guidance
Phase Field: Microstructural evolution
Nucleation, growth, diffusion
Continuum: Stress-strain curve, Fracture, Deformation

## Slide 19
DFT
Voltage Curves
Phase Stability
Crystal Structure
Molecular Dynamics: Lithium diffusion barriers
Li-conductivity pathways
Phase Field:
Thermal and Cycling Stress in Solid-State Battery Cathode

## Slide 20: LENGTH SCALES AND APPLICATIONS
 | Approx. Scale (m) | Example | Example Models
Macroscopic | > 10-3 | Behavior of components & devices | Finite Element Analysis (FEA), computational thermo
Mesoscopic | 10-6 - 10-3 | Polycrystals and their properties | FEA, phase field modeling, computational kinetics
Microscopic | 10-7 – 10-4 | Microstructure within a single crystal | Phase field modeling, computational kinetics, dislocation dynamics
Atomic | 10-9 - 10-6 | Fundamental mechanism for transport, deformation, etc. | Molecular dynamics
Quantum | 10-11 - 10-8 | Electronic structures, elastic constants, energetics | Density functional theory

## Slide 21
Cross-Industry Standard Process for Data Mining
(CRISP-DM)
Materials
Gathering Data from Materials Project

## Slide 22: Your Coding Experience? Python?
Data types (string, float, int, bool)
Print
If then, Boolean Operators (And, Not, Or)
For loop, While loop
Functions (modules)
Data structures: List, Dictionary
Plotting (Matplotlib)
Object-oriented programming?
Great Python
Introduction!

## Slide 23
Materials Project is a database
Application Programming Interface (API) is a query-engine for the data
Pymatgen is a python package to manipulate MP data

## Slide 24
Let’s design a class for a crystal structure
What kind of properties would you like to store?
What kind of actions would you like to perform?
variables
functions
Notes: Guide the class a little bit more with the attributes and such
e.g., point out the difference between zincblende and wurtzite

## Slide 25: Object Oriented Programming
Bank Account
Properties
Person: Object
Account Balance: Float
Account type (Checking/Saving): String
Person
Properties
Name: String
Address: String
Birthday: Date
Social Security Number: String
Password: String
Etc.
Functions
Add Funds
Withdraw Funds
Check Balance
Functions
Change Address
Change Password
https://www.geeksforgeeks.org/python-program-to-create-bankaccount-class-with-deposit-withdraw-function/

## Slide 27: Structure Class
Lattice
Species (elements/molecules, occupancies)
Fractional Coordinates
lattice:
species:
Coords(Nx3 array):
from pymatgen.core.structure import Structure
s = Structure(Lattice, Species, Coords)

## Slide 28: Structure Class
Contains:
Lattice – Set of lattice vectors
Species – List of species on each lattice site
Coords – List of fractional/cartesian coordinates for each species
Examples of Structure Class Methods:
Modify the structure
self.lattice()
self.append()
self.insert()
self.remove_sites()
self.translate_sites()
self.rotate_sites()
self.apply_strain()
self.calculate()
self.relax()
Perform a calculation

## Slide 29: Lattice class
Examples of Lattice Subclass Methods:
Modify the lattice
self.scale()
self.get_wigner_seitz_cell()
self.get_brillouin_zone()
self.get_miller_indices_from_coords()
Perform a calculation
self.lengths()
self.angles()
self.reciprocal_lattice()
self.inv_matrix()
Return lattice properties
Lattice = set of translation vectors to generate infinite periodic lattice
2D lattice vectors
Notes: An Animal object can be an attribute for a Zoo_area object
Similarly, a Lattice object can be an attribute for a Structure object

## Slide 30
Pymatgen is always changing and growing.
There is no great documentation, except the source code on Github
Explore it based on your MSE intuition. Start with core and analysis

## Slide 31
Professor Kioupakis asked me:
“I hypothesize that ionic oxides with high atomic density will have strong overlap of atomic orbitals, which will be correlated with a larger band gap.”
How might we explore this?

## Slide 33: Preparation for tomorrow:
Download and Install Anaconda
  https://www.anaconda.com/
Install Pymatgen
  Open Anaconda Prompt:
  Type: “conda install -c conda-forge pymatgen”
Open Anaconda Navigator
  Install Jupyter Notebook
  Try a few of the commands on the following page to see if Pymatgen is working properly: